## Slide 1: Enhanced Memory Properties in MIS TD by Forming Trench Structure at the Gate Edge
Presenter: Jian-Yu Lin1
Jian-Yu Lin1* , Jenn-Gwo Hwu1, 2
Graduate Institute of Electronics Engineering,
Department of Electrical Engineering, National Taiwan University, Taipei , Taiwan
Notes: Good morning everyone, my name is Jian-Yu Lin, from Nation Taiwan University. Today I’m going to talk about my research topic: “Enhanced Memory Properties in MIS TD by Forming Trench Structure at the Gate Edge”

## Slide 2: Outline
Introduction
  Metal-Insulator-Semiconductor (MIS) Tunnel Diode (TD)
  Memory Properties of MIS-TD
Device Structure and Fabrication
Results and Discussion
Conclusion
Notes: Here is my outline , first I will have a brief introduction of the physics and structure of Metal-insulator-semiconductor tunnel diode.
And its memory characteristics.
And then the fabrication process of my devices
followed by results and discussion
finally conclusion.

## Slide 3: Outline
Introduction
  Metal-Insulator-Semiconductor (MIS) Tunnel Diode (TD)
  Memory Properties of MIS-TD
Device Structure and Fabrication
Results and Discussion
Conclusion

## Slide 4: What is MIS Tunnel Diode?
Si (p)
SiO2
Diode-like I-V curve.
Al
Al
VG
MOS capacitor
SiO2
MIS tunnel diode (TD)
Direct
tunneling current
oxide thickness < 4 nm
Notes: MIS-TD is similar to Mos capacitor, except the oxide thickness is much more thinner so the electrons can directly tunnel through the oxide layer.
As a result, when we measure the I-V curve, we can get a diode-like I-V curve.
At negative voltage, MIS-TD has a large forward bias current
At positive voltage, MIS-TD has a smaller reverse bias saturation current

## Slide 5: MIS Tunnel Diode (Reverse Bias)
Fringing electric field > bulk electric field.
Saturation current mainly flow through gate edge.
At reverse bias
current flow
fringing field
Si (p)
SiO2
Al
Al
VG>0
depletion region
Notes: From our previous research, we know that at the reverse bias region the fringing electric field is larger than bulk electric field in MIS-TD.
Consequently, reverse bias saturation current mainly flow through device edge.
By utilizing this edge flowing saturation current And MIS-TDs have many applications such as
temperature sensor, light sensor and it also can be used as a memory device
-> so in the next page I will talk about how this MIS TD memory work.

## Slide 6: Memory Properties of MIS-TD
In previous work:
Apply negative and positive stress to MIS-TD.
Lower and higher current was measured.
2-state current phenomenon.
Reference: Tzu-Yu Chen et al., “Effect of Electrons Trapping/De-Trapping at Si-SiO2 Interface on Two-State Current in MOS(p) Structure with Ultra-Thin SiO2
by Anodization,“ ECS Journal of Solid State Science and Technology, 2 (9) Q159-Q164, 2013. DOI: 10.1149/2.025309jss
Potential for memory device use.
Notes: also In our previous work, we found that by applying –stress and +stress to the gate of the MIS TD,
we can manipulate the saturation current to 2 different levels, shown in the right figure -> which shows 2-state current characteristic .
This implies that MIS TD has the potential for memory device use

## Slide 7: In this work…
New structure of MIS-TD is proposed.
Si (p)
SiO2
Al
Al
VG
Conventional: Planar MIS
New Structure: Trench MIS
Al
Si (p)
SiO2
Al2O3
Al
VG
better memory properties.
Notes: In this work, we propose a new structure of MIS-TD, called Trench MIS.
Compared with conventional planar MIS structure, Trench MIS has a better memory properties.

## Slide 8: In this work…
Trench MIS TDs have better memory properties.
more obvious 2-state current.
10 times larger current window.
Current Window (CW)=
read current (after “Set”, open)- read current (after “Reset”, solid)
Current
Window
Current
Window
2-state current
Reset: -1.75V for 20s
Set: +1V for 10s
Notes: For example: in the following results and discussion section: we will show that endurance test
we read the current @0.2V after SET, RESET stress
the better memory properties means:
obvious 2-state current
10 times larger CW than planar MIS
and the current window is the read current difference between SET and RESET states.
** Planar current window=52 pA
Trench=650 pA

## Slide 9: Outline
Introduction
  Metal-Insulator-Semiconductor (MIS) Tunnel Diode (TD)
  Memory Properties of MIS-TD
Device Structure and Fabrication
Results and Discussion
Conclusion

## Slide 10: Device Structure and Fabrication
85 um
Al2O3
Al
85 um
SiO2
Al
Top view
Cross section
Planar MIS
Trench MIS
Effective oxide thickness (EOT)=2.5 nm
Planar MIS
SiO2
Si (p)
Al
Al
VG
Trench MIS
SiO2
Si (p)
500nm
Al
Al
VG
Al2O3
2.5nm
2.5nm
Notes: Here shows the top view and the cross section of the planar and trench MIS
And the depth of the trench is about 500nm
The oxide thickness is about 2.5nm

## Slide 11: Device Structure and Fabrication
p-type (100)-oriented silicon wafers with a resistivity of 1–10 Ω·cm
Radio Corporation of America (RCA) clean
Si (p)
Notes: first, we use a p-type silicon wafer as substrate and perform RCA clean

## Slide 12: Device Structure and Fabrication
Grow SiO2 by anodic oxidation
Radio Corporation of America (RCA) clean
Si (p)
SiO2
Notes: Grow SiO2 layer by anodic oxidation

## Slide 13: Device Structure and Fabrication
Grow SiO2 by anodic oxidation
Rapid thermal annealing (RTA) in N2 ambient @ 950 °C for 15 s.
Radio Corporation of America (RCA) clean
Si (p)
SiO2
Notes: and RTA

## Slide 14: Device Structure and Fabrication
Grow SiO2 by anodic oxidation
Rapid thermal annealing (RTA) in N2 ambient @ 950 °C for 15 s.
Deposit 200 nm Al by thermal evaporation
Radio Corporation of America (RCA) clean
Si (p)
SiO2
Al
Notes: Then we deposit 200nm Al by thermal evaporation as the top electrode

## Slide 15: Device Structure and Fabrication
Si (p)
SiO2
Al
PR
Circle structure patterned by photolithography
Notes: After that, we use photolithography to define our pattern

## Slide 16: Device Structure and Fabrication
Al
PR
Si (p)
SiO2
Circle structure patterned by photolithography
Etch Si substrate by reactive ion etch (RIE)
Notes: then we use PR as mask to perform RIE to form the trench structure.

## Slide 17: Device Structure and Fabrication
Al
PR
Si (p)
SiO2
Al2O3
Al2O3 layer:
protect Si substrate from being exposed to air.
Circle structure patterned by photolithography
Etch Si substrate by reactive ion etch (RIE)
Form a layer of Al2O3 : (1) thermal evaporate Al. (2) dip into nitric acid (HNO3) to oxidize Al.
Notes: because after RIE, the Si substrate is exposed to the air
we form a layer of Al2O3 To protect it.
this Al2O3 layer is formed by first evaporate a film of Al, and then oxidize Al by nitric acid.

## Slide 18: Device Structure and Fabrication
Al
Circle structure patterned by photolithography
Etch Si substrate by reactive ion etch (RIE)
Si (p)
SiO2
Form a layer of Al2O3 : (1) thermal evaporate Al. (2) dip into nitric acid (HNO3) to oxidize Al.
Al2O3
Lift-off PR
Al2O3 layer:
protect Si substrate from being exposed to air.
PR
Notes: we lift-off the PR

## Slide 19: Device Structure and Fabrication
Al
Circle structure patterned by photolithography
Etch Si substrate by reactive ion etch (RIE)
Si (p)
SiO2
Form a layer of Al2O3 : (1) thermal evaporate Al. (2) dip into nitric acid (HNO3) to oxidize Al.
Al2O3
Lift-off PR
Al
VG
Al2O3 layer:
protect Si substrate from being exposed to air.
removed backside native oxide by buffer oxide etchant (BOE)
200nm Al formed as back electrode by thermal evaporation
Notes: At last we form a 200nm Al as back electrode by thermal evaporation after we removed native oxide by BOE

## Slide 20: Outline
Introduction
  Metal-Insulator-Semiconductor (MIS) Tunnel Diode (TD)
  Memory Properties of MIS-TD
Device Structure and Fabrication
Results and Discussion
Conclusion

## Slide 21: I-V Curves: After Reset Stress
Al
Si (p)
SiO2
Al2O3
Al
Reset: VG<0
Al
Si (p)
SiO2
Al
Reset: VG<0
Apply -1.5V for 120s and then -1.75V for 20s to gate as “Reset” stress.
Measure I-V from -0.5V~0.5V (solid symbol).
Notes: At the beginning, we measure the I-V curves after Reset and Set stress.
we first apply negative voltage stress to the gate, which was used as RESET stress
and then we measure the I-V curve sweep from -0.5V~0.5V

## Slide 22: I-V Curves: After Set Stress
Al
Si (p)
SiO2
Al2O3
Al
Set: VG>0
Al
Si (p)
SiO2
Al
Set: VG>0
Apply +1V for 20s to gate as “Set” stress.
Measure I-V from +0.5V~-0.5V (open symbol).
Notes: After that, we apply positive stress to both planar and trench, which was used as SET stress
then measure current sweep from +0.5V~-0.5V as shown in the figure as open symbol.

## Slide 23: I-V Curves: 2-state Current
Al
Si (p)
SiO2
Al2O3
Al
Vread=0.2V
Al
Si (p)
SiO2
Al
Vread=0.2V
Trench MIS has a more obvious 2- state current phenomenon.
Notes: So in this figure, we can see Trench shows a more obvious 2-state current than planar,
which can be seen in the current difference of solid and open symbol @0.2V.

## Slide 24: Memory Endurance Measurement
3 endurance measurements with different “set stress”.
same reset stress.
read @VG=0.2V
each 50 cycles.
Notes: To Further examine the memory characteristics we measured 3 endurance tests.
For example: 1st endurance....

## Slide 25: Memory Endurance Results
Reset (solid), Set (open).
Trench MIS:
  stabler multi-level memory function.
  larger current window.
Current Window=
read current (after “Set”, open)- read current (after “Reset”, solid)
Notes: 3 endurance test are shown in this figure.
x-coordinate represent cycles number
y-coordinate represent read current @0.2V
under different stresses conditions: Trench MIS 4 different stable current levels compared with planar MIS
-> which shows trench MIS has multi-level memory function.
besides, Trench MIS has a larger current window (red solid and open sample)

## Slide 26: Electron Traps Mechanism: Reset
current flow
electron flow
fringing field
Al
Reset (-1.75V 20s), then Read “0”
Al
Al2O3
Si (p)
SiO2
e-
Vread =0.2V
depletion region
Reset: trap electrons
Electrons trap in Al2O3/SiO2 interface and SiO2 layer.
Notes: At the end, we propose a electron trap mechanism to explain why trench MIS has better memory properties.
first, we start from RESET stress operation:
  RESET traps electrons into the interface @the trench edge and SiO2 layer
  when we later read@0.2V, the electron appeal by the gate will see repulsive coulomb force stopping them from approaching gate.
  As a result, less electron can tunnel through gate and read current is small
.

## Slide 27: Electron Traps Mechanism: Set
current flow
electron flow
fringing field
Al
Set (+1V 10s), then Read “3”
Al
Si (p)
SiO2
e-
VG =0.2V
depletion region
Set: detrap electrons
Trench structure offers extra electron traps.
Better memory properties.
Notes: Then, we apply SET stress operation:
  which detraps electrons in the interface @the trench edge and SiO2 layer
  repulsive coulomb force is smaller
  As a result, more electron can tunnel through gate and read current is high
So why trench MIS has better memory properties is because it has more electron traps located @ trench edge.
Thus, can results a bigger change in coulomb force and thus bigger change in read current.

## Slide 28: Outline
Introduction
  Metal-Insulator-Semiconductor (MIS) Tunnel Diode (TD)
  Memory Properties of MIS-TD
Device Structure and Fabrication
Results and Discussion
Conclusion

## Slide 29: Conclusion
In this work, a new structure of MIS TD, trench MIS TD, is proposed.
Trench MIS TDs have better memory properties than planar MIS TD.
Electron trap mechanism : more electron traps offered by trench structure.
However, we still need more study to verify this mechanism.

## Slide 30: Thank you for listening !

## Slide 31: Q&A

## Slide 32: Anodic Oxidation (ANO)
Can be performed in room temperature, then RTA.
Uniform oxide layer.
Si2+ +2e- +2H2O →SiO2+2H2

## Slide 33: Functions of Al2O3 Layer
Functions of this layer:
  protect Si substrate from moisture and air.
  provide electron traps in Al2O3/Si interface.
Al
Si (p)
SiO2
Al2O3
Al
VG
e-

## Slide 34: Uniformity of Al2O3 layer
Evaporated Al oxidized by nitric acid.
The Al2O3 layer is non-uniform:
  may influence the moisture and air protection.
Solutions (different ways to form sidewall):
  Al2O3 sidewall: by sputter Al target in Ar/O2 ambient.
  SiO2 sidewall: by anodic oxidation.
Al
Si (p)
SiO2
Al
VG
2nd ANO SiO2
Al
Si (p)
SiO2
Al2O3
Al
VG
Notes: some part of the al oxide sidewall is too thin to protect the Si substrate from moisture and air.
So recently we tried to solve this problem by using different ways to form the sidewall

## Slide 35: Quality of Al2O3 Layer
Purpose of this layer: protect Si substrate from moisture and air.
Current window easily degrades.
might because the instability of native oxide.
Al
Si (p)
SiO2
Al
VG
native oxide
Prototype trench MIS (native oxide)
Al
Si (p)
SiO2
Al2O3
Al
VG
trench MIS in this work
Current window is more stable.
Acceptable quality of Al2O3 Layer.
but can be improved.

## Slide 36: Further Verification of the Mechanism
Trench structure offers electron traps at gate edge
More edge (by different mask pattern design).
Better current window.
Al
Al
Si (p)
SiO2
Al2O3
Al
VG
Top view:
Al

## Slide 37: Improvement of Stress Time
Currently, the “Reset” and “Set” stress time is still too long (>1s)
Possible ways to improve:
  increase the edge of the pattern under the same footprint.
  increase the depth of the trench structure.
  ∵ more edge or more trench → more electron traps.
Al
SiO2
Si (p)
500nm
Al
Al
VG
Al2O3