## Slide 1: Dependency of Transient Current Behavior on Oxide Thickness in Trench Structure MIS TDs
Presenter: Jian-Yu Lin
Jian-Yu Lin1* , Jenn-Gwo Hwu1, 2
Graduate Institute of Electronics Engineering,
Department of Electrical Engineering, National Taiwan University, Taipei , Taiwan
*Acknowledgement: this work was supported by the Ministry of Science and Technology of Taiwan under Contracts MOST 110-2221-E-002-140 and 110-2622-8-002-014
Notes: Good morning everyone, my name is Jian-Yu Lin, from Nation Taiwan University. Today I’m going to talk about “Dependency of Transient Current Behavior on Oxide Thickness in Trench Structure MIS TDs”
注意”So”語助詞

## Slide 2: Outline
Introduction
  Metal-Insulator-Semiconductor Tunnel Diode (MIS TD)
  Transient Current in MIS TDs
Results and Discussion
  Experiments
  TCAD Simulation
Conclusion
Notes: Here is my outline , first I will have a brief introduction about what is Metal-insulator-semiconductor tunnel diode and the transient current in this kind of device.
Second part is the results and discussion
followed by the conclusion.

## Slide 3: Outline
Introduction
  Metal-Insulator-Semiconductor Tunnel Diode (MIS TD)
  Transient Current in MIS TDs
Results and Discussion
  Experiments
  TCAD Simulation
Conclusion

## Slide 4: What is MIS TD?
Diode-like I–V curve.
VG < 0: forward bias region.
VG > 0: reverse bias region.
Si (p)
SiO2
Al
Al
VG
MOS capacitor
SiO2
MIS tunnel diode (TD)
Direct
tunneling current
oxide thickness
< 4 nm
*Metal-Insulator-Semiconductor (MIS)
*Metal-insulator-semiconductor tunnel diode (MIS TD)
Notes: MIS TD is an abbreviation for Metal-insulator-semiconductor tunnel diode (MIS TD).
it has almost the same device structure as MOS capacitor does.
Except, MIS TD has a thinner oxide thickness (usually smaller than 4 nm)
This allows MIS TD to have a large direct tunneling current.
So when we measure the I-V curves of the device, we can get a diode like I-V.

## Slide 5: What is MIS TD?
Diode-like I–V curve.
VG < 0: forward bias region.
VG > 0: reverse bias region.
Si (p)
SiO2
Al
Al
VG
MIS tunnel diode (TD)
Direct
tunneling current
oxide thickness
< 4 nm
*Metal-Insulator-Semiconductor (MIS)
*Metal-insulator-semiconductor tunnel diode (MIS TD)
Notes: MIS TD is an abbreviation for Metal-insulator-semiconductor tunnel diode (MIS TD).
it has almost the same device structure as MOS capacitor does.
Except, MIS TD has a thinner oxide thickness (usually smaller than 4 nm)
This allows MIS TD to have a large direct tunneling current.
So when we measure the I-V curves of the device, we can get a diode like I-V.

## Slide 6: Transient Current in MIS TDs
J. -Y. Lin and J. -G. Hwu, IEEE Transactions on Electron Devices 68, 4189-4194 (2021)
Trench MIS TDs
I-V more obvious hysteresis.
Stronger transient current.
Trench structure MIS (Trench MIS)
New special structure
Planar structure MIS (Planar MIS)
Normal structure
Notes: So our group has done a lot of research about MIS TDs.
And one of the research is the transient current in MIS TDs.
For example, in our previous work, we propose a new structure for MIS TDs. called Trench MIS.
Compared with normal structure MIS, in here we called it Planar MIS,
Trench MIS demonstrate a stronger transient current.
To elaborate, please look at this I-V curves.
If you focus on low voltage region.
For trench MIS (red lines), you can see the sweep forward and backward…….hysteresis
This indicate stronger transient current in Trench MIS.

## Slide 7: Transient Current in MIS TDs (cont.)
Transient current behavior
  Store two memory states.
Trench MIS TDs:
  potential for memory devices.
Endurance Property
J. -Y. Lin and J. -G. Hwu, IEEE Transactions on Electron Devices 68, 4189-4194 (2021)
Notes: In the same research, we demonstrated that this transient current can be used to store two different memory states.
And because of this
Trench MIS has the potential to be used as Memory devices

## Slide 8: In This Work…
Investigate the dependency of
transient current.
on the tunneling oxide thickness (dox)
Different dox
Experiment
Trench structure MIS (Trench MIS)
Notes: So in this work
we follow up the previous research in Trench MIS
we further investigate the dependency of transient current on the oxide thickness using exp. and simulation.
We believe this work can deepen our understanding about the transient current of Trench MIS devices.

## Slide 9: Outline
Introduction
  Metal-Insulator-Semiconductor Tunnel Diode (MIS TD)
  Transient Current in MIS TDs
Results and Discussion
  Experiments
  TCAD Simulation
Conclusion
Notes: now we come to the first experiments part in the results and discussion

## Slide 10: Device Structure
*Detailed fabrication process can be found in IEEE Transactions on Electron Devices 68, 4189-4194 (2021)
Notes: Here shows the top view and the cross section of the planar and trench MIS.
Detailed fabrication process can be found in our previous work.

## Slide 11: I-V Curves with Different dox
For Trench MIS, when dox 
  more apparent hysteresis.
  stronger transient current.
dox 
dox 
Notes: At the beginning, I want to first talk about the I-V curves with different dox
left figure show Planar with not transient current.
On the other hand, the right figure show the Trench MIS.
If we look at the color region,
when the dox thicker, transient current become stronger.

## Slide 12: Memory Retention Measurement
Solid: read “-1”.
For Trench MIS, when dox 
  Stronger transient current ( i.e. |read “-1” current| ).
Memory pulses
dox
Where does “transient current” come from?
Notes: This trend can be also observed in the memory retention property.
Apply memory pulses to the gate of MIS TD.
first is the write “-1” operation, which apply 2V for 1ms to the gate of the device.
And at read “-1” operation, we quickly switch the Vg to 0 V and read the gate current
Write 0, we apply a 0V to the gate, followed by read “0” operation to read the gate current.
See the right retention measurment. y-axis represent the read current.
horizontal axis represent time.
In this figure we can notice that read “0” signal are all close to 0 current line, so we can barely see the open symbol.
However, the read “-1” transient current would increase with oxide thickness.
In order to fully explain this trend, I have to first talk about where…

## Slide 13: The Origin of Read “-1” Transient Current
dox
Iread “–1” = (| Ie (T) |+| Ih (T) |) – (| Ie (D) |+| Ih (D) |)
Write “–1” (VG=2V)
Read “–1” (VG=0V)
*ninv : inversion carriers
*nexcess : excess electrons
| read “-1” current | ∝ nexcess ∝ ninv (@VG=2V)
⇒
*solid arrows: current flow
*nexcess ninv (@VG = +2V) – ninv (@VG = 0V)
Notes: First look at this band diagram of trench MIS。
This shows what happens when we apply a write “-1” pulse to the device.
As you can see, the 2 V Vg will attract inversion carriers to the interface.
After that gate voltage was quickly switch to 0 V to read the gate current.
Because the switching from 2V to 0V is so quick that the ninv attracted by 2 V gate voltage
don’t have time to be recombined or repelled at the beginning of read “-1” condition.
These inversion charges will become excess electrons, nexcess,
and cause the whole device under non-equilibrium state.
To return to equilibrium, the number of nexcess has to decrease.
So the process of nexcess decrease creates the transient current we observe in the left side retention figure.
To sum up, we can write down this relation
since the read “-1” current comes from the nexcess
it should be proportional to nexcess.
and the nexcess is proportional to the ninv @ 2V。

## Slide 14: dox and Transient Current
nexcess, 2 ↑
Pt, 2 ↓
tunneling probability (Pt)
−
−
−
−
−
−
−
ninv, 2 ↑
+2V
3.05 nm (thick)
nexcess, 1 ↓
+2V
Pt, 1 ↑
−
−
−
ninv, 1 ↓
2.6 nm (thin)
Al
SiO2
Si (p)
Pt, 1 > Pt, 2
ninv, 1 < ninv, 2
nexcess, 1 < nexcess, 2
| read “-1” | 1 < | read “-1” | 2
| read “-1” current | ∝ nexcess ∝ ninv (@VG=2V)
dox
Notes: Using this relation, we can now came back to explain the dox and read “-1” current relation.
Please look at the right-side band diagram.
For thick oxide sample, because the device will have smaller oxide tunneling probability Pt
At 2 V, thick oxide device can accumulate more ninv, and also more nexcess.
And because read “-1” current is proportional to nexcess, thick oxide device should have stronger transient current.

## Slide 15: Outline
Introduction
  Metal-Insulator-Semiconductor Tunnel Diode (MIS TD)
  Transient Current in MIS TDs
Results and Discussion
  Experiments
  TCAD Simulation
Conclusion

## Slide 16: Silvaco TCAD Simulation Setting
Fig. Simulated structure of Trench MIS.
Fig. Silvaco TCAD simulation process.
dox = 2.5 ~ 3 nm
  dox ↑, |read “-1” current| ↑.
TCAD Simulation
dox > 3 nm (simulation)
  dox ↑, |read “-1” current| ↓.
Two trends of dox — transient current
Notes: Top figure show the simulated device structure.
bottom figure show the simulation process.
Basically, we simulated write “-1” to read “-1” operations.
And the simulated results are shown on the right-side.
y-axis…x-axis
if you give a closer look at this figure, you can notice there are two different trends of dox-transient current
in here, I mark with two different colors.
in yellow part, the transient current increase with dox
However, when dox become too thick, in the green region,
we can notice the transient current will start to decrease.
So in order to explain these two trends,
in the following, I will split this figure into two different parts to discuss about it.
at first, I want to talk about the yellow part
不能解釋兩區差異

## Slide 17: Simulated Retention: Part 1
dox = 2.5 ~ 3 nm
  dox ↑, |read “-1” current| ↑.
TCAD Simulation
dox
Experiment
Trench MIS TDs
dox
dox ↑ » nexcess ↑ » |read “-1” current| ↑
Notes: The first part….
the trend align well with our previous experiment results on the right side
And in the previous part, we argue that this is because dox increase, nexcess will increase……
So now we are going to use TCAD to prove that when doX increase, the nexcess will increase too.

## Slide 18: Simulated Retention: Part 1
dox = 2.5 ~ 3 nm
  dox ↑, |read “-1” current| ↑.
nexcess at t= 1.35 ms (simulation)
dox ↑
Pt ↓
ninv ↑
nexcess ↑
TCAD Simulation
dox
*dox ↑ » nexcess ↑ » |read “-1” current| ↑
Notes: I draw the simulated nexcess into two contour plots, shown on the right.
You can notice when the dox increase, nexcess increase too
according to our explanation in the experimental part.
This is because…..
This leads to the larger transient current observed in the simulation results.
Therefore, TCAD results prove our previous explanation.

## Slide 19: Simulated Retention: Part 2
dox = 2.5 ~ 3 nm
  dox ↑, |read “-1” current| ↑.
nexcess at t= 1.35 ms (simulation)
dox ↑ ↑
Cox ↓
ninv ↓
nexcess ↓
dox > 3 nm (simulation)
  dox ↑, |read “-1” current| ↓.
dox
| read “-1” current | ∝ nexcess
TCAD Simulation
Notes: However, in the simulation, we also observe an opposite trend in simulation, when dox is thicker than 3 nm.
That is, the read “-1” transient current would decrease with the increasing dox.
In order to explain this trend, we also extract the nexcess
We found that when dox become too thick, it will result in the decrease of Cox, and resulting in the device to hold fewer ninv, and nexcess.
So this explain why transient current will start to decrease when the dox become too thick.

## Slide 20: Outline
Introduction
  Metal-Insulator-Semiconductor Tunnel Diode (MIS TD)
  Transient Current in MIS TDs
Results and Discussion
  Experiments
  TCAD Simulation
Conclusion
Notes: 這是今天的outline，大概分為幾個部分，

## Slide 21: Conclusion
Investigated “transient current – dox“ relation of Trench MIS TDs by (1) experiments and (2) TCAD simulation.
dox = 2.5 ~ 3 nm: dox ↑, Pt ↓, nexcess ↑, |Transient current| ↑.
dox = 3 ~ 5 nm: dox ↑, Cox ↓, nexcess ↓, |Transient current| ↓.
|Transient current| ∝ excess electrons (nexcess).
Notes: As a brief summary of this work, we found that transient current is proportional to nexcess.

## Slide 22: Thank you for listening!
Presenter: Jian-Yu Lin
Graduate Institute of Electronics Engineering
National Taiwan University

## Slide 23: Acknowledgement
This work was supported by the Ministry of Science and Technology of Taiwan under Contracts MOST 110-2221-E-002-140 and 110-2622-8-002-014.

## Slide 24: Q&A

## Slide 25: Memory Retention
dox

## Slide 26: Turn Around in Experiment
Y-axis: Current Window ≈ |read “-1” current |.
X-axis: dox from 3.25 ~ 2.45 nm.
dox

## Slide 27: Transient TCAD with Different EOTs
Electron concentration under linear scale (different dox)

## Slide 28: TCAD Simulation: Models
Physical Models
1. Concentration-dependent mobility (conmob)
2. SRH (srh)
3. Auger (auger)
4. Band gap narrowing (bgn)
5. Field-dependent mobility (fldmob)
6. Quantum/direct tunneling (qtunnsc)
7. Bohm quantum potential (bqp) models
consider distribution of electrons in the inversion layer (quantum confinement)
Notes: print印出解的過程，transient使用model相同，method不同 (Gummel + Newton vs. quasi-static + Newton method)

## Slide 29: TCAD and Experiment (Different Time Scale)
TCAD: time = 1 ~ 30 ms.
  limited by the simulation time (may be several days).
  improvements are needed in the future work.
Experiment: time = 65 ms ~ 4 s.
dox
Experiment
Trench MIS TDs
dox

## Slide 30: Trench Structure

## Slide 31: Lower Oxide Electric Field in Trench MIS (TCAD)
Device structure
Contour plot of total electric field
Notes: 也因此可以驗證我們剛剛的解釋: 也就是trench的反偏壓電流較小，就是來自於他的oxide跨壓較小所造成的

## Slide 32: Anodic Oxidation (ANO) System
Jun-Yao Chen, “Effect of Compensatory Embedded Aluminum on the Electrical Characteristics of MIS Tunnel Diode with Ultrathin Oxide” Master thesis, Graduate Institute of Electronics Engineering, College of Electrical Engineering and Computer Science, National Taiwan University 2016.

## Slide 33: Effect of Passivation Layer
SiO2 sidewall devices are more unstable.
SiO2 (ANO)

## Slide 34: dox-Dependency of I–V Curves
Oxide tunneling limited
Minority carriers supply limited
EFp
| Ih1 |
Vox1
Thick Oxide
+2V
Al
SiO2
Si (p)
+2V
EFp
| Ih2 |
Vox2
Thin Oxide
Vox1 > Vox2
<
| Ih1 | > | Ih2 |
dox , Vox  , , and | Ih | .
C. Liao, W. Kao, and J. Hwu, IEEE Journal of the Electron Devices Society, vol. 4, no. 6, pp. 424-429, 2016, doi: 10.1109/JEDS.2016.2591956.

## Slide 35: Perimeter-Dependencies of I–V Curves
Edge flowing current dominant at VG > 0 [∵ Fringing field effect (Eedge)].
Eedge > Ebulk .
Vox,edge > Vox,bulk .
< .
Ih,edge > Ih,bulk.

## Slide 36: Device Structure
Notes: Here shows the top view and the cross section of the planar and trench MIS

## Slide 37: Device Fabrication (1/2)
Radio Corporation of America (RCA) clean
Si (p)
Ultra-thin oxide grown by anodic oxidation
RTA in N2 at 950 ⁰C for 15 s
Thermal evaporate 250nm Al as top electrode
Photolithography
Al wet etching
Si substrate etching by RIE
Notes: first, we use a p-type silicon wafer as substrate and perform RCA clean

## Slide 38: Device Fabrication (1/2)
Radio Corporation of America (RCA) clean
Ultra-thin oxide grown by anodic oxidation
Rapid thermal annealing (RTA) in N2 at 950 ⁰C for 15 s
Si (p)
SiO2
Thermal evaporate 250nm Al as top electrode
Photolithography
Al wet etching
Si substrate etching by RIE
Notes: Grow SiO2 layer by anodic oxidation
followed by RTA

## Slide 39: Device Fabrication (1/2)
Radio Corporation of America (RCA) clean
Ultra-thin oxide grown by anodic oxidation
RTA in N2 at 950 ⁰C for 15 s
Thermal evaporate 250nm Al as top electrode
Si (p)
SiO2
Al
Photolithography
Al wet etching
Si substrate etching by RIE
Notes: Then we deposit 200nm Al by thermal evaporation as the top electrode

## Slide 40: Device Fabrication (1/2)
Radio Corporation of America (RCA) clean
Ultra-thin oxide grown by anodic oxidation
RTA in N2 at 950 ⁰C for 15 s
Thermal evaporate 250nm Al as top electrode
Photolithography
Si (p)
SiO2
Al
PR
Al wet etching
Si substrate etching by RIE
Notes: After that, we use photolithography to define our pattern

## Slide 41: Device Fabrication (1/2)
Radio Corporation of America (RCA) clean
Ultra-thin oxide grown by anodic oxidation
RTA in N2 at 950 ⁰C for 15 s
Thermal evaporate 250nm Al as top electrode
Photolithography
Al wet etching
SiO2
Al
PR
Si (p)
Si substrate etching by RIE
Trench MIS only process
Notes: then we use PR as mask to perform RIE to form the trench structure.

## Slide 42: Device Fabrication (2/2)
SiO2
Al
PR
Si (p)
Al2O3
Remove native oxide by BOE
Deposit Al2O3 by in-situ oxidation of dc sputtering Al target in Ar/O2 ambient
Lift-off photoresist (PR)
Furnace annealing in N2 at 200 ⁰C for 10 minutes
Backside native oxide removal
200 nm Al back electrode deposition
Al2O3 layer (passivation layer):
protect Si substrate from being exposed to air.
Notes: because after RIE, the Si substrate is exposed to the air
we form a layer of Al2O3 To protect it.
this Al2O3 layer is formed by DC sputtering.

## Slide 43: Device Fabrication (2/2)
SiO2
Al
Si (p)
Lift-off photoresist (PR)
Furnace annealing in N2 at 200 ⁰C for 10 minutes
Backside native oxide removal
200 nm Al back electrode deposition
Deposit Al2O3 by in-situ oxidation of dc sputtering Al target in Ar/O2 ambient
Remove native oxide by BOE
Al2O3
Notes: we lift-off the PR
and perform furnace annealing to improve the quality of al2O3

## Slide 44: Device Fabrication (2/2)
SiO2
Al
Si (p)
Backside native oxide removal
200 nm Al back electrode deposition
VG
Al
Lift-off photoresist (PR)
Furnace annealing in N2 at 200 ⁰C for 10 minutes
Deposit Al2O3 by in-situ oxidation of dc sputtering Al target in Ar/O2 ambient
Remove native oxide by BOE
Al2O3
Notes: At last we form a 200nm Al as back electrode by thermal evaporation after we removed native oxide by BOE